D 6483 MACK T-9

RING/LINER WEAR TEST

REPORT PACKET VERSION NO.  19981110

CONDUCTED FOR:

# TSTSPON1

# TSTSPON2

| LABVALID | V = VALID; THE REFERENCE OIL/NON-REFERENCE OIL WAS EVALUATED IN ACCORDANCE WITH THE TEST PROCEDURE. |
| --- | --- |
|  | I = INVALID; THE REFERENCE OIL/NON-REFERENCE OIL WAS NOT EVALUATED IN ACCORDANCE WITH THE TEST PROCEDURE. |
|  | N = RESULTS CANNOT BE INTERPRETED AS REPRESENTATIVE OF OIL PERFORMANCE (NON-REFERENCE OIL) AND SHALL NOT BE USED IN DETERMINING AN AVERAGE TEST RESULT USING MULTIPLE TEST CRITERIA. |

| STAND: STAND | STAND RUN NO.: RSTRUN/STRUN | ENGINE NO.: ENGINE | ENGINE HOURS: RENHOURS/ENHOURS |
| --- | --- | --- | --- |
| END OF TEST DATE: RDTCOMP/DTCOMP | END OF TEST TIME: EOTTIME/REOTTIME |
| OIL CODE/CMIR A: CMIR/OILCODE |
| FORMULATION/STAND CODE: FORM |
| ALTCODE1: ALTCODE1 | ALTCODE2: ALTCODE2 | ALTCODE3: ALTCODE3 |

In my opinion this test OPVALID been conducted in a valid manner in accordance with Test Method D 6483 and the appropriate amendments through the information letter system. The remarks included in this report describe the anomalies associated with this test.

| SUBMITTED BY: | SUBLAB |
| --- | --- |
|  | Testing Laboratory |
|  | SUBSIGIM |
|  | Signature |
|  | SUBNAME |
|  | Typed Name |
|  | SUBTITLE |
|  | Title |

D 6483 MACK T-9

RING/LINER WEAR TEST

### FORM 1 - NON-REFERENCE OIL TEST SUMMARY

| FORMULATION/STAND CODE FORM TEST LENGTH TESTLEN |
| --- |
| OIL CODE NO. OILCODE |
| TEST LAB | TEST STAND NO. | TEST STAND RUN NO. | ENGINE BLOCK SERIAL NO. | ENGINE HOURS |
| LAB | STAND | STRUN | ENGINE | ENHOURS |
| DATE TEST STARTED: | DTSTRT |
| START TIME: | STRTTIME |
| DATE TEST COMPLETED: |  | DTCOMP |
| EOT TIME: | EOTTIME |
| STAND CALIBRATION EXPIRATION DATE: | DTCALEXP |
| LABORATORY OIL CODE | LABOCODE |
| SAE VISCOSITY | SAEVISC |

| AVERAGE TGA SOOT % AT 75 h | TGAAVG |
| --- | --- |
| AVERAGE TGA SOOT % 75 – 500 h | SOOTAVG |
| AVERAGE OIL CONSUMPTION (0.304 g/Kw-h max.) | OILCON |
| CENTRIFUGAL OIL FILTER MASS GAIN, g | MASSG |
| OIL FILTER DELTA P, kPa (138 max.) | XOILDP |
| EOT TBN | TBN500 |

|  | DELTA Pb @ EOT (ppm) | ADJUSTED AVG. LINER WEAR (µm) | AVG. TOP RING WEIGHT LOSS (mg) |
| --- | --- | --- | --- |
| ORIGINAL RESULT | DPBEOT | ALW | ATRWL |
| TRANSFORMED RESULT A | TRNDPB |  |  |
| CORRECTION FACTOR A | DPBCF | ALWCF | ATRWLCF |
| CORRECTED TRANSFORMED RESULT A | DPBCOR | ALWCOR | ATRWLCOR |
| SEVERITY ADJUSTMENT A | DPB_SA | CLW_SA | ATRWL_SA |
| FINAL TRANSFORMED RESULT A | TDPBFNL | TCLWFNL | TTRWLFNL |
| FINAL ORIGINAL UNIT RESULT | DPBFNL | CLWFNL | ATRWLFNL |

D 6483 MACK T-9

RING/LINER WEAR TEST

### FORM 1A - REFERENCE OIL TEST SUMMARY

| CMIR CODE NO. CMIR TEST LENGTH TESTLEN |
| --- |
| TMC OIL NO. IND |
| TEST LAB | TEST STAND NO. | TEST STAND RUN NO. | ENGINE BLOCK SERIAL NO. | ENGINE HOURS |
| LAB | STAND | RSTRUN | RENGINE | RENHOURS |
| DATE TEST STARTED: |  | RDTSTRT |
| START TIME: | RSTRTTIME |
| DATE TEST COMPLETED: |  | RDTCOMP |
| EOT TIME: | REOTTIME |
| STAND CALIBRATION EXPIRATION DATE: | RDTCALEXP |
| LABORATORY OIL CODE | RLABOCODE |
| SAE VISCOSITY | RSAEVISC |

| AVERAGE TGA SOOT % AT 75 h | RTGAAVG |
| --- | --- |
| AVERAGE TGA SOOT % 75 – 500 h | RSOOTAVG |
| AVERAGE OIL CONSUMPTION (0.304 g/Kw-h max.) | ROILCON |
| CENTRIFUGAL OIL FILTER MASS GAIN, g | RMASSG |
| OIL FILTER DELTA P, kPa (138 max.) | RXOILDP |
| EOT TBN | RTBN500 |

|  | DELTA Pb @ EOT (ppm) | ADJUSTED AVG. LINER WEAR (µm) | AVG. TOP RING WEIGHT LOSS (mg) |
| --- | --- | --- | --- |
| ORIGINAL RESULT | RDPBEOT | RALW | RATRWL |
| TRANSFORMED RESULT A | RTRNDPB |  |  |
| CORRECTION FACTOR A | DPBCF | ALWCF | ATRWLCF |
| FINAL TRANSFORMED RESULT A | RTDPBFNL | RTCLWFNL | RTTRWLFNL |
| FINAL ORIGINAL UNIT RESULT | RDPBFNL | RCLWFNL | RATRWLFNL |

D 6483 MACK T-9

RING/LINER WEAR TEST

Operational Summary

FORM 2

| Laboratory: LAB | EOT Date: RTDTCOMP/DTCOMP | EOT Time: EOTTIME/REOTTIME |
| --- | --- | --- |
| Test Number:STAND - RSTRUN/STRUN - ENGINE - ENRUN/RENRUNCMIR/OILCODE |
| Oil Code: |
| Formulation/Stand Code: FORM |

| Controlled Parameters | Parameter | Units | QI Threshold | EOT QI A | Target | Average | Samples B | BQD C | Over/Under Range D |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Speed | r/min | 0.000 | QRPM | 1800 | 1250 | ARPMA | ARPMB | NRPM | BRPM | ORPM |
|  | Fuel Flow | kg/h | 0.000 | QFFLO | 63.28 | 55.00 | AFFLOA | AFFLOB | NFFLO | BFFLO | OFFLO |
|  | Coolant Out | °C | 0.000 | QCOLOUT | 85 | ACOLOUT | NCOLOUT | BCOLOUT | OCOLOUT |
|  | Fuel In | °C | 0.000 | QFUELT | 40 | AFUELT | NFUELT | BFUELT | OFUELT |
|  | Oil Gallery | °C | 0.000 | QOILTEM | 25 | AOILTEM | NOILTEM | BOILTEM | OOILTEM |
|  | Intake Manifold | °C | 0.000 | QINMANT | 43 | AINMANTA AINMANTB | NINMANT | BINMANT | OINMANT |
|  | Exhaust | kPa | 0.000 | QEXHSTP | 3.1 | AEXHSTP | NEXHSTP | BEXHSTP | OEXHSTP |
|  | Inlet Air Res. | KPa | 0.000 | QINAIRR | 2.5 | AINAIRR | NINAIRR | BINAIRR | OINAIRR |
| Non-controlled Parameters | Parameter | Units | Typical Values E | Average |  |
|  | Torque | N-m | 1361 - 1457 | 2118 - 2208 | ALOAD1 | ALOAD2 |  |
|  | Power | kW | 258 - 267 | 280 - 288 | APWR1 | APWR2 |  |
|  | Humidity | g/kg | 4.2 – 78.6 | AHUMID |  |
|  | Blowby | L/min | 41.2 – 184.3 | 23.6 – 148.7 | ABLOBY1 | ABLOBY2 |  |
|  | Coolant In | °C | 76 - 82 | ACOLIN |  |
|  | Oil Gallery | °C | 101 - 109 | AOILT |  |
|  | Pre-Turb. (F) | °C | 605 - 658 | APTURFT |  |
|  | Pre-Turb. (R) | °C | 613 - 674 | APTURRT |  |
|  | Tailpipe | °C | 428 - 474 | 514 – 559 | ATAILPT1 | ATAILPT2 |  |
|  | Oil Gallery | kPa | 365 - 436 | 227-284 | AOILPRS1 | AOILPRS2 |  |
|  | Crankcase | kPa | 0.27 – 0.60 | ACCASEP |  |
|  | Intake Manifold | kPa | 185 – 201 | 149 – 164 | AINMANP1 | AINMANP2 |  |
|  | Compressor Discharge | kPa | 193 - 205 | 152 - 159 | ACOMDIS1 | ACOMDIS2 |  |
|  | Intercooler Delta | kPa | 13.6 Maximum | AINCLDP |  |

### D 6483 MACK T-9

RING/LINER WEAR TEST

### Rod Bearing Weight Loss

Form 3

| Laboratory: LAB | EOT Date: RTDTCOMP/DTCOMP | EOT Time: EOTTIME/REOTTIME |
| --- | --- | --- |
| Test Number: STAND - RSTRUN/STRUN - ENGINE - ENRUN/RENRUN CMIR/OILCODE |
| Oil Code: |
| Formulation/Stand Code: FORM |

| Cylinder # | Location | SOT Weight, g | EOT Weight, g | Weight Change, mg |
| --- | --- | --- | --- | --- |
| 1 | Upper | BWSOTU1 | BWEOTU1 | BWLU1 |
| 2 | Upper | BWSOTU2 | BWEOTU2 | BWLU2 |
| 3 | Upper | BWSOTU3 | BWEOTU3 | BWLU3 |
| 4 | Upper | BWSOTU4 | BWEOTU4 | BWLU4 |
| 5 | Upper | BWSOTU5 | BWEOTU5 | BWLU5 |
| 6 | Upper | BWSOTU6 | BWEOTU6 | BWLU6 |

| SUMMARY | As Measured | Outlier Screened |
| --- | --- | --- |
| Upper Bearing Average Weight Loss, mg | ABWLU | OABWLU |
| Upper Bearing Weight Loss Std. Dev., mg | SBWLU | OSBWLU |
| Upper Bearing Minimum Weight Loss, mg | IBWLU | OIBWLU |
| Upper Bearing Maximum Weight Loss, mg | XBWLU | OXBWLU |
| Outlier Upper Rod Bearing A | BWLOUT |  |

A Cylinder number

| Cylinder # | Location | SOT Weight, g | EOT Weight, g | Weight Change, mg |
| --- | --- | --- | --- | --- |
| 1 | Lower | BWSOTL1 | BWEOTL1 | BWLL1 |
| 2 | Lower | BWSOTL2 | BWEOTL2 | BWLL2 |
| 3 | Lower | BWSOTL3 | BWEOTL3 | BWLL3 |
| 4 | Lower | BWSOTL4 | BWEOTL4 | BWLL4 |
| 5 | Lower | BWSOTL5 | BWEOTL5 | BWLL5 |
| 6 | Lower | BWSOTL6 | BWEOTL6 | BWLL6 |
| Upper Bearing Average Weight Loss, mg |  | ABWLL |
| Upper Bearing Weight Loss Std. Dev., mg |  | SBWLL |
| Upper Bearing Minimum Weight Loss, mg |  | IBWLL |
| Upper Bearing Maximum Weight Loss, mg |  | XBWLL |

### D 6483 MACK T-9

RING/LINER WEAR TEST

Ring Weight Loss

Form 4

| Laboratory: LAB | EOT Date: RTDTCOMP/DTCOMP | EOT Time: EOTTIME/REOTTIME |
| --- | --- | --- |
| Test Number: STAND - RSTRUN/STRUN - ENGINE - ENRUN/RENRUN CMIR/OILCODE |
| Oil Code: |
| Formulation/Stand Code: FORM |

| Cylinder # | Top Ring SOT Weight, g | Top Ring EOT Weight, g | Weight Loss, mg |
| --- | --- | --- | --- |
| 1 | TRWSOT1 | TRWEOT1 | TRWL1 |
| 2 | TRWSOT2 | TRWEOT2 | TRWL2 |
| 3 | TRWSOT3 | TRWEOT3 | TRWL3 |
| 4 | TRWSOT4 | TRWEOT4 | TRWL4 |
| 5 | TRWSOT5 | TRWEOT5 | TRWL5 |
| 6 | TRWSOT6 | TRWEOT6 | TRWL6 |

| SUMMARY | As Measured | Outlier Screened |
| --- | --- | --- |
| Upper Bearing Average Weight Loss, mg | AMATRWL | ATRWL |
| Upper Bearing Weight Loss Std. Dev., mg | AMSTRWL | STRWL |
| Upper Bearing Minimum Weight Loss, mg | AMITRWL | ITRWL |
| Upper Bearing Maximum Weight Loss, mg | AMXTRWL | XTRWL |
| Outlier Ring B | OUTTR |
| Top Rings with Plasma Flaking C | FLKTR |

A Results calculated without rings with plasma flanking.

B Ring number wear results are not currently outlier screened.

C Ring numbers: 1,2, etc. separated by commas. Example: 2,3,5

| Cylinder # | 2nd Ring SOT Weight, g | 2nd Ring EOT Weight, g | Weight Loss, mg |
| --- | --- | --- | --- |
| 1 | R2WSOT1 | R2WEOT1 | R2WL1 |
| 2 | R2WSOT2 | R2WEOT2 | R2WL2 |
| 3 | R2WSOT3 | R2WEOT3 | R2WL3 |
| 4 | R2WSOT4 | R2WEOT4 | R2WL4 |
| 5 | R2WSOT5 | R2WEOT5 | R2WL5 |
| 6 | R2WSOT6 | R2WEOT6 | R2WL6 |
|  | 2nd Ring Average Weight Loss, mg | AR2WL |
|  | 2nd Ring Weight Loss Std. Dev., mg | SR2WL |
|  | 2nd Ring Min. Weight Loss, mg | IR2WL |
|  | 2nd Ring Max. Weight Loss, mg | XR2WL |

| Cylinder # | 2nd Ring SOT Weight, g | 2nd Ring EOT Weight, g | Weight Loss, mg |
| --- | --- | --- | --- |
| 1 | ORWSOT1 | ORWEOT1 | ORWL1 |
| 2 | ORWSOT2 | ORWEOT2 | ORWL2 |
| 3 | ORWSOT3 | ORWEOT3 | ORWL3 |
| 4 | ORWSOT4 | ORWEOT4 | ORWL4 |
| 5 | ORWSOT5 | ORWEOT5 | ORWL5 |
| 6 | ORWSOT6 | ORWEOT6 | ORWL6 |
|  | Oil Ring Average Weight Loss, mg | AORWL |
|  | Oil Ring Weight Loss Std. Dev., mg | SORWL |
|  | Oil Ring Minimum Weight Loss, mg | IORWL |
|  | Oil Ring Maximum Weight Loss, mg | XORWL |

D 6483 MACK T-9

RING/LINER WEAR TEST

Oil Analysis Summary

### Form 5

| Laboratory: LAB | EOT Date: RTDTCOMP/DTCOMP | EOT Time: EOTTIME/REOTTIME |
| --- | --- | --- |
| Test Number: STAND - RSTRUN/STRUN - ENGINE - ENRUN/RENRUN CMIR/OILCODE |
| Oil Code: |
| Formulation/Stand Code: FORM |

| HOURS | SOOT Wt.% TGA | Viscosity At 100◦C cSt | Viscosity Increase cSt | TBN Annex A7 | TBN D2896 | TAN Annex A8 | Metals in Parts per Millions |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  | Elements |
|  |  |  |  |  |  |  | Fe | Pb | Cu | Cr | Al | Si | Sn | Na |
| NEWTST_H000 | TGA_H000 | V100H000 |  | TBN_H000 | TAN_H000 | IRINH000 | FEWMH000 | PBWMH000 | CUWMH000 | CRWMH000 | ALWMH000 | SIWMH000 | SNWMH000 | NAWMH000 |
| TST_H025 | TGA_H025 | V100H025 | IVISH025 | TBN_H025 | TAN_H025 | IRINH025 | FEWMH025 | PBWMH025 | CUWMH025 | CRWMH025 | ALWMH025 | SIWMH025 | SNWMH025 | NAWMH025 |
| TST_H050 | TGA_H050 | V100H050 | IVISH050 | TBN_H050 | TAN_H050 | IRINH050 | FEWMH050 | PBWMH050 | CUWMH050 | CRWMH050 | ALWMH050 | SIWMH050 | SNWMH050 | NAWMH050 |
| TST_H075 | TGA_H075 | V100H075 | IVISH075 | TBN_H075 | TAN_H075 | IRINH075 | FEWMH075 | PBWMH075 | CUWMH075 | CRWMH075 | ALWMH075 | SIWMH075 | SNWMH075 | NAWMH075 |
| TST_H752 | TGA75_2 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 75 AVG | RTGAAVG/TGAAVG |  |  |  |  |  |  |  |  |  |  |  |  |  |
| TST_H100 | TGA_H100 | V100H100 | IVISH100 | TBN_H100 | TAN_H100 | IRINH100 | FEWMH100 | PBWMH100 | CUWMH100 | CRWMH100 | ALWMH100 | SIWMH100 | SNWMH100 | NAWMH100 |
| TST_H150 | TGA_H150 | V100H150 | IVISH150 | TBN_H150 | TAN_H150 | IRINH150 | FEWMH150 | PBWMH150 | CUWMH150 | CRWMH150 | ALWMH150 | SIWMH150 | SNWMH150 | NAWMH150 |
| TST_H200 | TGA_H200 | V100H200 | IVISH200 | TBN_H200 | TAN_H200 | IRINH200 | FEWMH200 | PBWMH200 | CUWMH200 | CRWMH200 | ALWMH200 | SIWMH200 | SNWMH200 | NAWMH200 |
| TST_H250 | TGA_H250 | V100H250 | IVISH250 | TBN_H250 | TAN_H250 | IRINH250 | FEWMH250 | PBWMH250 | CUWMH250 | CRWMH250 | ALWMH250 | SIWMH250 | SNWMH250 | NAWMH250 |
| TST_H300 | TGA_H300 | V100H300 | IVISH300 | TBN_H300 | TAN_H300 | IRINH300 | FEWMH300 | PBWMH300 | CUWMH300 | CRWMH300 | ALWMH300 | SIWMH300 | SNWMH300 | NAWMH300 |
| TST_H350 | TGA_H350 | V100H350 | IVISH350 | TBN_H350 | TAN_H350 | IRINH350 | FEWMH350 | PBWMH350 | CUWMH350 | CRWMH350 | ALWMH350 | SIWMH350 | SNWMH350 | NAWMH350 |
| TST_H400 | TGA_H400 | V100H400 | IVISH400 | TBN_H400 | TAN_H400 | IRINH400 | FEWMH400 | PBWMH400 | CUWMH400 | CRWMH400 | ALWMH400 | SIWMH400 | SNWMH400 | NAWMH400 |
| TST_H425 |  |  |  |  |  |  |  | PBWMH425 |  |  |  |  |  |  |
| TST_H450 | TGA_H450 | V100H450 | IVISH450 | TBN_H450 | TAN_H450 | IRINH450 | FEWMH450 | PBWMH450 | CUWMH450 | CRWMH450 | ALWMH450 | SIWMH450 | SNWMH450 | NAWMH450 |
| TST_H475 |  |  |  |  |  |  |  | PBWMH475 |  |  |  |  |  |  |
| TST_H500 | TGA_H500 | V100H500 | IVISH500 | TBN_H500 | TAN_H500 | IRINH500 | FEWMH500 | PBWMH500 | CUWMH500 | CRWMH500 | ALWMH500 | SIWMH500 | SNWMH500 | NAWMH500 |

| Summary | As Measured | Outlier Bearing Adjusted |
| --- | --- | --- |
| Delta Pb @ EOT, ppm | AMDPBEOT | RDPBEOT/DPBEOT |

### D 6483 MACK T-9

RING/LINER WEAR TEST

Liner Surface Roughness & Bore Diameter

Form 6

| Laboratory: LAB | EOT Date: RTDTCOMP/DTCOMP | EOT Time: EOTTIME/REOTTIME |
| --- | --- | --- |
| Test Number: STAND - RSTRUN/STRUN - ENGINE - ENRUN/RENRUN CMIR/OILCODE |
| Oil Code: |
| Formulation/Stand Code: FORM |

| LINER NO. | LOCATION | Ra (µm) | BORE DIAMETER (mm) |  | Ra (µm) | DIA. (mm) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Top Ring Travel @ 0◦C | LIN1RAA | LIN1IDA | AVG | ALIN1RA | ALIN1ID |
|  | Top Ring Travel @ 90◦C | LIN1RAB | LIN1IDB | STD DEV | SLIN1RA |  |
|  | Top Ring Travel @ 180◦C | LIN1RAC |  | MIN | ILIN1RA |  |
|  | Top Ring Travel @ 270◦C | LIN1RAD |  | MAX | XLIN1RA |  |

| 2 | Top Ring Travel @ 0◦C | LIN2RAA | LIN2IDA | AVG | ALIN2RA | ALIN2ID |
| --- | --- | --- | --- | --- | --- | --- |
|  | Top Ring Travel @ 90◦C | LIN2RAB | LIN2IDB | STD DEV | SLIN2RA |  |
|  | Top Ring Travel @ 180◦C | LIN2RAC |  | MIN | ILIN2RA |  |
|  | Top Ring Travel @ 270◦C | LIN2RAD |  | MAX | XLIN2RA |  |

| 3 | Top Ring Travel @ 0◦C | LIN3RAA | LIN3IDA | AVG | ALIN3RA | ALIN3ID |
| --- | --- | --- | --- | --- | --- | --- |
|  | Top Ring Travel @ 90◦C | LIN3RAB | LIN3IDB | STD DEV | SLIN3RA |  |
|  | Top Ring Travel @ 180◦C | LIN3RAC |  | MIN | ILIN3RA |  |
|  | Top Ring Travel @ 270◦C | LIN3RAD |  | MAX | XLIN3RA |  |

| 4 | Top Ring Travel @ 0◦C | LIN4RAA | LIN4IDA | AVG | ALIN4RA | ALIN4ID |
| --- | --- | --- | --- | --- | --- | --- |
|  | Top Ring Travel @ 90◦C | LIN4RAB | LIN4IDB | STD DEV | SLIN4RA |  |
|  | Top Ring Travel @ 180◦C | LIN4RAC |  | MIN | ILIN4RA |  |
|  | Top Ring Travel @ 270◦C | LIN4RAD |  | MAX | XLIN4RA |  |

| 5 | Top Ring Travel @ 0◦C | LIN5RAA | LIN5IDA | AVG | ALIN5RA | ALIN5ID |
| --- | --- | --- | --- | --- | --- | --- |
|  | Top Ring Travel @ 90◦C | LIN5RAB | LIN5IDB | STD DEV | SLIN5RA |  |
|  | Top Ring Travel @ 180◦C | LIN5RAC |  | MIN | ILIN5RA |  |
|  | Top Ring Travel @ 270◦C | LIN5RAD |  | MAX | XLIN5RA |  |

| 6 | Top Ring Travel @ 0◦C | LIN6RAA | LIN6IDA | AVG | ALIN6RA | ALIN6ID |
| --- | --- | --- | --- | --- | --- | --- |
|  | Top Ring Travel @ 90◦C | LIN6RAB | LIN6IDB | STD DEV | SLIN6RA |  |
|  | Top Ring Travel @ 180◦C | LIN6RAC |  | MIN | ILIN6RA |  |
|  | Top Ring Travel @ 270◦C | LIN6RAD |  | MAX | XLIN6RA |  |

|  | Ra (µm) | BORE DIAMETER (mm) |
| --- | --- | --- |
| Average Surface Roughness & Bore Diameter | ALINRA | ALINID |
| Standard Deviation Surface Roughness & Bore Diameter | SLINRA | SLINID |
| Minimum Surface Roughness & Bore Diameter | ILINRA | ILINID |
| Maximum Surface Roughness & Bore Diameter | XLINRA | XLINID |

D 6483 MACK T-9

RING/LINER WEAR TEST

### Liner Wear Summary

Form 7

| Laboratory: LAB | EOT Date: RTDTCOMP/DTCOMP | EOT Time: EOTTIME/REOTTIME |
| --- | --- | --- |
| Test Number: STAND - RSTRUN/STRUN - ENGINE - ENRUN/RENRUN CMIR/OILCODE |
| Oil Code: |
| Formulation/Stand Code: FORM |

| POSITION | WEAR STEP (µm) |
| --- | --- |
|  | Cylinder Number |
|  | 1 | 2 | 3 | 4 | 5 | 6 |
| 1:00 | C1LW1 | C2LW1 | C3LW1 | C4LW1 | C5LW1 | C6LW1 |
| 2:00 | C1LW2 | C2LW2 | C3LW2 | C4LW2 | C5LW2 | C6LW2 |
| 3:00 (Thrust) | C1LW3 | C2LW3 | C3LW3 | C4LW3 | C5LW3 | C6LW3 |
| 4:00 | C1LW4 | C2LW4 | C3LW4 | C4LW4 | C5LW4 | C6LW4 |
| 5:00 | C1LW5 | C2LW5 | C3LW5 | C4LW5 | C5LW5 | C6LW5 |
| 6:00 (Rear) | C1LW6 | C2LW6 | C3LW6 | C4LW6 | C5LW6 | C6LW6 |
| 7:00 | C1LW7 | C2LW7 | C3LW7 | C4LW7 | C5LW7 | C6LW7 |
| 8:00 | C1LW8 | C2LW8 | C3LW8 | C4LW8 | C5LW8 | C6LW8 |
| 9:00 (Anti-Thrust) | C1LW9 | C2LW9 | C3LW9 | C4LW9 | C5LW9 | C6LW9 |
| 10:00 | C1LW10 | C2LW10 | C3LW10 | C4LW10 | C5LW10 | C6LW10 |
| 11:00 | C1LW11 | C2LW11 | C3LW11 | C4LW11 | C5LW11 | C6LW11 |
| 12:00 (Front) | C1LW12 | C2LW12 | C3LW12 | C4LW12 | C5LW12 | C6LW12 |
| Average | C1ALW | C2ALW | C3ALW | C4ALW | C5ALW | C6ALW |

| Summary | As Measured | Outlier Screened | Adjusted to 1.75% Soot |
| --- | --- | --- | --- |
| Average, µm | AMACLW | ALW | RALW/ALWALW |
| Std. Dev., µm | AMSCLW | SCLW | SCLW |
| Minimum, µm | AMICLW | ICLW | ICLW |
| Maximum, µm | AMXCLW | ZCLW | ZCLW |
| Ring Flaked Outliers B | FLKLIN | ZCLW |
| Outlier Liners C | OUTLIN | ZCLW |

A Do not use data from liners with top ring plasma flaking for determining “As Measured” result.

B Cylinder Number: 1,2, etc. separated by commas. Example: 2,3

C  Cylinder Number.

D 6483 MACK T-9

RING/LINER WEAR TEST

Unscheduled Downtime & Maintenance Summary

### Form 8

| Laboratory: LAB | EOT Date: RTDTCOMP/DTCOMP | EOT Time: EOTTIME/REOTTIME |
| --- | --- | --- |
| Test Number: STAND - RSTRUN/STRUN - ENGINE - ENRUN/RENRUN CMIR/OILCODE |
| Oil Code: |
| Formulation/Stand Code: FORM |

| Number of Downtime Occurrences | DWNOCR |  |
| --- | --- | --- |
| Test Hours | Date | Downtime | Reasons |
| DOWNH001 | DDATH001 | DTIMH001 | DREAH001 |
|  |  | TOTLDOWN | Total Downtime (hours) |

| Other Comments |  |
| --- | --- |
| Number of Comment Lines | TOTCOM |  |
| OCOMH001 |

D 6483 MACK T-9

RING/LINER WEAR TEST

Unscheduled Downtime & Maintenance Summary

### Form 8A

| Laboratory: LAB | EOT Date: RTDTCOMP/DTCOMP | EOT Time: EOTTIME/REOTTIME |
| --- | --- | --- |
| Test Number: STAND - RSTRUN/STRUN - ENGINE - ENRUN/RENRUN CMIR/OILCODE |
| Oil Code: |
| Formulation/Stand Code: FORM |

| Number of Downtime Occurrences | DWNOCR |  |
| --- | --- | --- |
| Test Hours | Date | Downtime | Reasons |
| DOWNH001 | DDATH001 | DTIMH001 | DREAH001 |
|  |  | TOTLDOWN | Total Downtime (hours) |

| Other Comments |  |
| --- | --- |
| Number of Comment Lines | TOTCOM |  |
| OCOMH001 |

D 6483 MACK T-9

RING/LINER WEAR TEST

Unscheduled Downtime & Maintenance Summary

### Form 8B

| Laboratory: LAB | EOT Date: RTDTCOMP/DTCOMP | EOT Time: EOTTIME/REOTTIME |
| --- | --- | --- |
| Test Number: STAND - RSTRUN/STRUN - ENGINE - ENRUN/RENRUN CMIR/OILCODE |
| Oil Code: |
| Formulation/Stand Code: FORM |

| Number of Downtime Occurrences | DWNOCR |  |
| --- | --- | --- |
| Test Hours | Date | Downtime | Reasons |
| DOWNH001 | DDATH001 | DTIMH001 | DREAH001 |
|  |  | TOTLDOWN | Total Downtime (hours) |

| Other Comments |  |
| --- | --- |
| Number of Comment Lines | TOTCOM |  |
| OCOMH001 |

D 6483 MACK T-9

RING/LINER WEAR TEST

Test Fuel Analysis (Last Batch)

### Form 9

| Laboratory: LAB | EOT Date: RTDTCOMP/DTCOMP | EOT Time: EOTTIME/REOTTIME |
| --- | --- | --- |
| Test Number: STAND - RSTRUN/STRUN - ENGINE - ENRUN/RENRUN CMIR/OILCODE |
| Oil Code: |
| Formulation/Stand Code: FORM |
| Supplier: FUELSUP | Batch Identifiers: FUELBTID |

| Measurement | Specs. | Analysis | Test Method |
| --- | --- | --- | --- |
|  |  | NEW | EOT |  |
| Total Sulfur, % Weight | 0.03 – 0.05 | FUELSNEW | FUELSEOT | D 2622 |
| Gravity, ◦API | 32 – 36 | APIGRNEW | APIGREOT | D 287 or D 4052 |
| Hydrocarbon Composition |  |  |  |
| Aromatics % Vol. | 28 – 35 | FUELAROM | D 1319 |
| Olefin | Report | FUELOFF | D 1319 |
| Saturates | Report | FUELSATU | D 1319 |
| Cetane Index | Report | CETANEIN | D 976 & D 4737 |
| Cetane No. | 42 – 48 | CETANENO | D 613 |
| Copper Strip Corrosion | 1 Maximum | FUELCU | D 130 |
| Flash Point, ◦C | 54 Minimum | FUELSHPT | D 93 |
| Cloud Point, ◦C | -12 Maximum | FUELCLOU | D 2500 |
| Pour Point, ◦C | -18 Maximum | FUELPOUR | D 97 |
| Carbon Residue on 10% Residuum, % | 0.35 Maximum | FUELCRES | D 524 (10% Bottoms) |
| Water & Sediment, % Vol. | 0.05 Maximum | FUELH2O | D 2709 |
| Ash, % Wgt. | 0.01 Maximum | FUELASH | D 482 |
| Viscosity, cSt @ 40◦C | 2.0 – 3.2 | KINVIS | D 445 |
| Distillation, ◦C |  |  |  |
| IBP | 177-199 | FUELIBP | D 86 |
| 10% | 210-232 | FUEL10 | D 86 |
| 50% | 249-277 | FUEL50 | D 86 |
| 90% | 299-327 | FUEL90 | D 86 |
| EP | 327-360 | FUELEP | D 86 |

D 6483 MACK T-9

RING/LINER WEAR TEST

Characteristics of the Data Acquisition System

### Form 10

| Laboratory: LAB | EOT Date: RTDTCOMP/DTCOMP | EOT Time: EOTTIME/REOTTIME |
| --- | --- | --- |
| Test Number: STAND - RSTRUN/STRUN - ENGINE - ENRUN/RENRUN CMIR/OILCODE |
| Oil Code: |
| Formulation/Stand Code: FORM |

| PARAMETER (1) | SENSING DEVICE (2) | CALIBRATION FREQUENCY (3) | RECORD DEVICE (4) | OBSERVATION FREQUENCY (5) | RECORD FREQUENCY (6) | LOG FREQUENCY (7) | SYSTEM RESPONSE (8) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Temperatures |  |  |  |  |  |  |  |
| Oil @ Filt. | OTEMSENS | OTEMCALF | OTEMRECD | OTEMOBSF | OTEMRECF | OTEMLOGF | OTEMSYSR |
| Fuel In. | FTEMSENS | FTEMCALF | FTEMRECD | FTEMOBSF | FTEMRECF | FTEMLOGF | FTEMSYSR |
| Intake Air | AITSENS | AITCALF | AITRECD | AITOBSF | AITRECF | AITLOGF | AITSYSR |
| Intake Man. | IMANSENS | IMANCALF | IMANRECD | IMANOBSF | IMANRECF | IMANLOGF | IMANSYSR |
| Pre-Turb. | PTURSENS | PTURCALF | PTURRECD | PTUROBSF | PTURRECF | PTURLOGF | PTURSYSR |
| Cool. Out | COTSENS | COTCALF | COTRECD | COTOBSF | COTRECF | COTLOGF | COTSYSR |
| Other |  |  |  |  |  |  |  |
| Fuel Flow | FFLOSENS | FFLOCALF | FFLORECD | FFLOOBSF | FFLORECF | FFLOLOGF | FFLOSYSR |
| Engine RPM | RPMSENS | RPMCALF | RPMRECD | RPMOBSF | RPMRECF | RPMLOGF | RPMSYSR |
| Load | LOADSENS | LOADCALF | LOADRECD | LOADOBSF | LOADRECF | LOADLOGF | LOADSYSR |
| Inlet Restr. | INRESENS | INRECALF | INRERECD | INREOBSF | INRERECF | INRELOGF | INRESYSR |
| Exh. Press. | EXPRSENS | EXPRCALF | EXPRRECD | EXPROBSF | EXPRRECF | EXPRLOGF | EXPRSYSR |
| Oil Gal. Press. | OILGSENS | OILGCALF | OILGRECD | OILGOBSF | OILGRECF | OILGLOGF | OILGSYSR |

LEGEND:

(1) 	Operating Parameter

(2) 	The type of device used to measure temperature, pressure or flow

(3) 	Frequency at which the measurement system is calibrated

(4) 	The type of device where data is recorded

LG - Handlog Sheet

DL - Automatic Data Logger

SC - Strip Chart Recorder

C/M - Computer, Using Manual Data Entry

C/D - Computer, Using Direct I/O Entry

(5) 	Data are observed but only if recorded off spec.

(6) 	Data are recorded but are not retained at EOT

(7) 	Data are logged as permanent record, note specify if:

SS - Snapshot Taken at Specified Frequency

AG/X - Average of X Data Points at Specified Frequency

(8) 	Time for the output to reach 63.2% of final value for step change at input

D 6483 MACK T-9

RING/LINER WEAR TEST

Build-up and Hardware Information

Form 11

| Laboratory: LAB | EOT Date: RTDTCOMP/DTCOMP | EOT Time: EOTTIME/REOTTIME |
| --- | --- | --- |
| Test Number: STAND - RSTRUN/STRUN - ENGINE - ENRUN/RENRUN CMIR/OILCODE |
| Oil Code: |
| Formulation/Stand Code: FORM |

STATIC INJECTION TIMING

| Timing Hours | Timing (Deg) |
| --- | --- |
| SITHR001 | SIT_R001 |
| TOTSIT | Total Timing Changes |

HARDWARE

| Part | Part Number | Serial Number |
| --- | --- | --- |
| Injection Pump | INJPMPPN | INJPMPSN |
| Secondary Charger | TRBCHSPN |  |
| Cylinder Head (front) | CYLHFRPN | CYLHFRSN |
| Cylinder Head (rear) | CYLHRRPN | CYLHRRSN |
| Pistons | PISTONPN |  |
| Injection Nozzles | INJNOZPN |  |
| Rod Bearings | RODBRGPN |  |
| Liners | LINERPN |  |
| Ring Set | RINGSTPN |  |

| Cylinder Kit Location | CPD ID Number |
| --- | --- |
| Cylinder 1 | CPDIDC1 |
| Cylinder 2 | CPDIDC2 |
| Cylinder 3 | CPDIDC3 |
| Cylinder 4 | CPDIDC4 |
| Cylinder 5 | CPDIDC5 |
| Cylinder 6 | CPDIDC6 |

D 6483 MACK T-9

RING/LINER WEAR TEST

Build-up and Hardware Information

Form 11A

| Laboratory: LAB | EOT Date: RTDTCOMP/DTCOMP | EOT Time: EOTTIME/REOTTIME |
| --- | --- | --- |
| Test Number: STAND - RSTRUN/STRUN - ENGINE - ENRUN/RENRUN CMIR/OILCODE |
| Oil Code: |
| Formulation/Stand Code: FORM |

STATIC INJECTION TIMING

| Timing Hours | Timing (Deg) |
| --- | --- |
| SITHR001 | SIT_R001 |
| TOTSIT | Total Timing Changes |

HARDWARE

| Part | Part Number | Serial Number |
| --- | --- | --- |
| Injection Pump | INJPMPPN | INJPMPSN |
| Secondary Charger | TRBCHSPN |  |
| Cylinder Head (front) | CYLHFRPN | CYLHFRSN |
| Cylinder Head (rear) | CYLHRRPN | CYLHRRSN |
| Pistons | PISTONPN |  |
| Injection Nozzles | INJNOZPN |  |
| Rod Bearings | RODBRGPN |  |
| Liners | LINERPN |  |
| Ring Set | RINGSTPN |  |

| Cylinder Kit Location | CPD ID Number |
| --- | --- |
| Cylinder 1 | CPDIDC1 |
| Cylinder 2 | CPDIDC2 |
| Cylinder 3 | CPDIDC3 |
| Cylinder 4 | CPDIDC4 |
| Cylinder 5 | CPDIDC5 |
| Cylinder 6 | CPDIDC6 |

D 6483 MACK T-9

RING/LINER WEAR TEST

Build-up and Hardware Information

Form 11B

| Laboratory: LAB | EOT Date: RTDTCOMP/DTCOMP | EOT Time: EOTTIME/REOTTIME |
| --- | --- | --- |
| Test Number: STAND - RSTRUN/STRUN - ENGINE - ENRUN/RENRUN CMIR/OILCODE |
| Oil Code: |
| Formulation/Stand Code: FORM |

STATIC INJECTION TIMING

| Timing Hours | Timing (Deg) |
| --- | --- |
| SITHR001 | SIT_R001 |
| TOTSIT | Total Timing Changes |

HARDWARE

| Part | Part Number | Serial Number |
| --- | --- | --- |
| Injection Pump | INJPMPPN | INJPMPSN |
| Secondary Charger | TRBCHSPN |  |
| Cylinder Head (front) | CYLHFRPN | CYLHFRSN |
| Cylinder Head (rear) | CYLHRRPN | CYLHRRSN |
| Pistons | PISTONPN |  |
| Injection Nozzles | INJNOZPN |  |
| Rod Bearings | RODBRGPN |  |
| Liners | LINERPN |  |
| Ring Set | RINGSTPN |  |

| Cylinder Kit Location | CPD ID Number |
| --- | --- |
| Cylinder 1 | CPDIDC1 |
| Cylinder 2 | CPDIDC2 |
| Cylinder 3 | CPDIDC3 |
| Cylinder 4 | CPDIDC4 |
| Cylinder 5 | CPDIDC5 |
| Cylinder 6 | CPDIDC6 |

D 6483 MACK T-9

RING/LINER WEAR TEST

Form 12

American Chemistry Council Code of Practice

Test Laboratory Conformance Statement

| Test Laboratory |  |
| --- | --- |
| Test Sponsor |  |
| Formulation / Stand Code |  |
| Test Number | TESTNUM |
| Start Date |  | Start Time |  | Time Zone |  |

Declarations

No. 1	All requirements of the ACC Code of Practice for which the test laboratory is responsible were met in the conduct of this test.     Yes__________     No__________*

No. 2	The laboratory ran this test for the full duration following all procedural requirements; and all operational validity requirements of the latest version of the applicable test procedure (ASTM or other) including all updates issued by the organization responsible for the test, were met.

Yes__________     No__________*

If the response to this Declaration is “No”, does the test engineer consider the deviations from operational validity requirements that occurred to be beyond the control of the laboratory?

Yes__________*    No__________

No. 3	A deviation occurred for one of the test parameters identified by the organization responsible for the test as being a special case. Yes__________*     No__________  (This currently applies only to specific deviations identified in the ASTM Information Letter System)

Check The Appropriate Conclusion

|  | Operational review of this test indicates that the results should be included in the Multiple Test Acceptance Criteria calculations. |
| --- | --- |
|  | *Operational review of this test indicates that the results should not be included in the Multiple Test Acceptance Criteria calculations. |

Note: Supporting comments are required for all responses identified with an asterisk.

Comments

___________________________________                               ____________________________________

Signature		Date

___________________________________                               ____________________________________

Typed Name		Title

# Text boxes

A CMIR or Non-Reference Oil Code

A Delta Pb Value in Transformed Units

A Delta Pb Value in Transformed Units

A Q1 values above the threshold are acceptable by the Mack Surveillance Panel.  QI values below the threshold may not be considered acceptable based on an engineering review. Refer to Annex A5

B Total number of data points taken. Minimum acceptable value is 3000

C Number of Bad Quality Data points not used in the calculation of the statistical measures.

D  Number of points clipped by over/under range limits.

E Typical values determined from reference oil test database