Two-Stroke-Cycle Gasoline Engine Lubricant Evaluation

D4857 (Y350M2) ASTM TC Sequence I Test Procedure

Title / Validity Declaration Page

Form 1

Version 20020830 BETA

Conducted for

### TSTSPON1

TSTSPON2

| LABVALID | I = Invalid |
| --- | --- |
|  | V =Valid |

| TSTOIL | NR = Non-Reference Test Oil |
| --- | --- |
|  | RO = Reference Oil Result |

| Test Number |
| --- |
| Engine No. ENGINE | Engine Run ENRUN |
| EOT Time EOTTIME | EOT Date DTCOMP |
| Reference Oil CMIR CYLROCDE | Cylinder |
| Non Reference Oil OILCODE CYLOILCD | Cylinder |
| Formulation/Stand FORM |
| Alternate Codes | ALTCODE1 | ALTCODE2 | ALTCODE3 |

In my opinion this test OPVALID been conducted in accordance with the Test Method D4857 and the appropriate amendments through information letter system. The remarks included in this report describe the anomalies with this test.

| SUBMITTED BY: | SUBLAB |
| --- | --- |
|  | Testing Laboratory |
|  | SUBSIGIM |
|  | Signature |
|  | SUBNAME |
|  | Typed Name |
|  | SUBTITLE |
|  | Title |

Two-Stroke-Cycle Gasoline Engine Lubricant Evaluation D4857 (Y350M2) ASTM TC Sequence I Test Procedure Table of Contents

Form 2

| Lab LAB | EOT Date DTCOMP | End Time EOTTIME |
| --- | --- | --- |
| Engine No. ENGINE | Run Number ENRUN |
| Reference Oil CMIR CYLROCDE | Cylinder |
| Non Reference Oil OILCODE CYLOILCD | Cylinder |
| Formulation / Stand Code FORM |

Form No.

Title / Validity Declaration Page	1

Table of Contents	2

Objective / Summary of Procedure	3

Objective / Summary of Procedure (continued)	3a

Test Result Summary	4

Ring Land Ratings	5

Ring Ratings	6

Operational Summary	7

Comments Summary	8

Air Fuel Ratio Plots	9

Spark Plug Plots	10

Fuel Analysis	11

Two-Stroke-Cycle Gasoline Engine Lubricant Evaluation

D4857 (Y350M2) ASTM TC Sequence I Test Procedure

Objective / Summary of Procedure

Form 3

Objective

This procedure is designed to evaluate the performance of a two-cycle engine lubricant relative to engine cleanliness when tested in a two-cylinder motorcycle engine. Particular attention will be given to the following characteristics.

1.	Piston Skirt Varnish

2.	Piston Ring Sticking

3.	Spark Plug Fouling

4.	Pre-ignition

5.	Combustion Chamber Deposits

6.	Exhaust Port Blocking

Summary of Procedure

The engine selected for this evaluation is a Yamaha RD350B air-cooled, two cylinder, two-cycle engine with the following specifications:

Displacement	21.18 cu. in. (347 cm3 )

Cylinder Bore	2.250 in. (64 mm)

Stroke	2.126 in. (54 mm)

Compression Ratio	6.6:1

Piston/ Cylinder Clearance         0.004 in.

1st Oversized Pistons

The separate cylinder arrangement of this engine, with individual intake and exhaust systems for each cylinder, allows an evaluation of the benchmark reference oil and non-reference oil simultaneously.

A 2-h break-in is completed before the test begins, At the start of test and prior to each cycle, the engine is idled for five min. The transmission is in fourth gear during testing. The test operates on the following cyclic schedule:

Phase I	Phase II

Engine, r/min	220 ± 200	6000 ± 5

Engine, bhp	0	8.5 ± 0.5 Air /

Fuel Ratio	----	12.0 ± 0.20 Spark Plug Gasket Temp.,   ° F	Record	375 ± 5

Exhaust Temp.,   ° F	Record	Approx. 1240 ± 140 Duration, min.	5	25

This is repeated five times for 150 min. test time.

The engine is then shut down for a minimum of 60 min. to complete one cycle.

This cycle is repeated eight times for a total running time of 20-h .

Two-Stroke-Cycle Gasoline Engine Lubricant Evaluation

D4857 (Y350M2) ASTM TC Sequence I Test Procedure

Objective / Summary of Procedure

Form 3a (continued)

The Data Acquisition System used to support this test operation meets the Automated Systems requirements Phase I data is sampled every 10s and 6 data points are averaged during the last minute of Phase I to provide a reading. Phase II data is sampled every 10s and 112 data points are averaged during the last eighteen min. to provide a reading. All parameters are acquired and averaged by the Automated Data Acquisition System.

At the conclusion of the test, the engine is disassembled, examined and rated (according to appropriate CRC manuals).

At the June 22, 1999 Section D02.B0.06 meeting, the Section agreed to change the reference oil, used as both the calibration and benchmark reference oil from TMC 600 to TMC 606. Since this reference oil performs differently than the previous benchmark reference oil on second ring sticking, the Section also approved the implementation of a correction factor of -2.45 merits to be applied to the benchmark reference oil (TMC 606) second ring sticking results, when run with the non-reference oil. The correction factor was adjusted from -2.45 to -1.85 at the June 2000 Section D02.B0.06 meeting.

The following are the criteria for non-reference oil approval purposes:

In the test two runs are normally made, exchanging the oils between cylinders after the 20 h run, and the means of the ratings for the non-reference and benchmark reference oils are compared. A pass may be given to the non-reference oil without making the second run if the following conditions all exist after the first run:

Piston varnish rating for the non-reference oil is equal to or better than the benchmark reference oil.

Second ring sticking merit rating for the non-reference oil are 9.0 or better.

No incidence of pre-ignition.

Not more than one incident of plug fouling with the non-reference oil.

Exhaust port blocking for the non-reference oil is not more than 5% greater than for the benchmark reference oil.

No scuffing or other lubricant related damage.

When the cross-over run must be made, the following conditions apply:

Piston Skirt-Varnish - The mean piston varnish rating of a non-reference oil shall be not more than 0.5 point below that of the benchmark reference oil.

Ring Sticking- The mean rating of the second rings of the non-reference oil pistons shall be not more than 0.5 point below that of the benchmark reference oil.

Pre-ignition - Any occurrence of pre-ignition in the non-reference oil cylinder shall constitute a failure.

Spark Plug Fouling - Not more than two more occurrences per complete test (2 runs) with the non-reference oil than with the benchmark reference oil.

Exhaust Port Blocking- The percentage of the exhaust port area blocked by deposits in either run of the test shall not be more than 10% greater for the non-reference oil than for the benchmark reference oil.

Two-Stroke-Cycle Gasoline Engine Lubricant Evaluation

D4857 (Y350M2) ASTM TC Sequence I Test Procedure

## Test Result Summary

## Form 4

| Lab LAB | EOT Date DTCOMP | End Time EOTTIME |
| --- | --- | --- |
| Engine No. ENGINE | Run Number ENRUN |
| Reference Oil CMIR CYLROCDE | Industry Oil Code IND | Cylinder |
| Non Reference Oil OILCODE CYLOILCD | Cylinder |
| Formulation / Stand Code FORM |

| Date Test DTSTRT | Start Time STRTTIME |
| --- | --- |
| Stand No. STAND | Test Length TESTLEN |

| Test Information |
| --- |
| Cylinder Number | CYLROCDE | CYLOILCD |
| Laboratory Oil | RLABCODE | LABOCODE |
| Fuel Type | RFUEL | FUEL |
| Fuel / Oil Ratio | RFUELRAT | FUELRAT |

| Engine Inspection |
| --- |
| Cylinder Number | CYLROCDE | CYLOILCD |
| Piston Varnish | Thrust | RPVTHR | PVTHR |
|  | Anti-Thrust | RPVATHR | PVATHR |
|  | Average | RAVGPV | AVGPV |
|  | Ring Land | RPVRNGL | PVRNGL |
|  | Undercrown | RPVUC | PVUC |
| Wristpin | Varnish | RWPVARN | WPVARN |
|  | Condition | RWPCOND | WPCOND |
|  | Bearing Varnish | RWPBVARN | WPBVARN |
|  | Bearing Condition | RWPBCOND | WPBCOND |
| Cylinder Liner Varnish | RCYLVARN | CYLVARN |
| Ring Sticking | Top Ring | RRSTOPRG | RSTOPRG |
|  | Second Ring | RRS2RG | RS2RG |
|  | -2.45 Correction Factor | RRSCOR | RSCOR |
| Deposits | Piston Crown | RPCCARB | PCCARB |
|  | Cylinder Head | RCHCARB | CHCARB |
|  | Exhaust Port Blocking % | REXHPBP | EXHPBP |
| Piston Scuffing | Thrust | RPSTHR | PSTHR |
|  | Anti-Thrust | RPSATHR | PSATHR |
| Cylinder Liner Wear | RCLWR | CLWR |
| CRC Demerit Number | Ring Land | RCRCRL | CRCRL |

Two-Stroke-Cycle Gasoline Engine Lubricant Evaluation

D4857 (Y350M2) ASTM TC Sequence I Test Procedure

Ring Land Ratings

Form 5

| Lab LAB | EOT Date DTCOMP | End Time EOTTIME |
| --- | --- | --- |
| Engine No. ENGINE | Run Number ENRUN |
| Reference Oil CMIR CYLROCDE | Industry Oil Code IND | Cylinder |
| Non Reference Oil OILCODE CYLOILCD | Cylinder |
| Formulation / Stand Code FORM |

| Ring Lands - Carbon Ratings |
| --- |
| Cylinder Number | CYLROCDE | CYLOILCD |
| Deposit Type | Deposit Factor | Area % | Demerit | Area % | Demerit |
| HC | 1.000 | RHCCCARB | RHCDEM | HCCCARB | HCDEM |
| MHC | 0.750 | RMHCCARB | RMHCDEM | MHCCARB | MHCDEM |
| MC | 0.500 | RMCCARB | RMCDEM | MCCARB | MCDEM |
| LC | 0.250 | RLCCARB | RLCDEM | LCCARB | LCDEM |
| VLC | 0.150 | RVLCCARB | RVLCDEM | VLCCARB | VLCDEM |
| Carbon Rating (demerits) | RCRBDTOT | CRBDTOT |

| Ring Lands - Lacquer Ratings |
| --- |
| Cylinder Number | CYLROCDE | CYLOILCD |
| Deposit Type | Deposit Factor | Area % | Demerit | Area % | Demerit |
| BL | 0.100 | RBLVARN | RBLDEM | BLVARN | BLDEM |
| DBRN | 0.075 | RDBRVARN | RDBRDEM | DBRVARN | DBRDEM |
| AL | 0.050 | RALVARN | RALDEM | ALVARN | ALDEM |
| LAL | 0.025 | RLALVARN | RLALDEM | LALVARN | LALDEM |
| VLAL | 0.010 | RVLAVARN | RVLADEM | VLAVARN | VLADEM |
| RL | 0.001 | RRLVARN | RRLDEM | RLVARN | RLDEM |
| Lacquer Rating | RVRNDTOT | VRNDTOT |
| Clean | 0 | RRLCLNA | RRLCLND | RLCLNA | RLCLND |

| Zonal Rating (demerits) | RCRCRL | CRCRL |
| --- | --- | --- |

Two-Stroke-Cycle Gasoline Engine Lubricant Evaluation

D4857 (Y350M2) ASTM TC Sequence I Test Procedure

Ring Ratings

Form 6

| Lab LAB | EOT Date DTCOMP | End Time EOTTIME |
| --- | --- | --- |
| Engine No. ENGINE | Run Number ENRUN |
| Reference Oil CMIR CYLROCDE | Industry Oil Code IND | Cylinder |
| Non Reference Oil OILCODE CYLOILCD | Cylinder |
| Formulation / Stand Code FORM |

| Cylinder Number | Ring Number | NMMA Rating | -1.85 Correction Factor A | Visual Rating | Adjusted Rating B |
| --- | --- | --- | --- | --- | --- |
| RCYLND1 | RRINGNO1 | RNMMA1 | RCF1 | RVR1 | RAR1 |
| RCYLND2 | RRINGNO2 | RNMMA2 | RCF2 | RVR2 | RAR2 |
| RCYLND3 | RRINGNO3 | RNMMA3 | RCF3 | RVR3 | RAR3 |
| CYLND1 | RINGNO1 | NMMA1 | CF1 | VR1 | AR1 |
| CYLND2 | RINGNO2 | NMMA2 | CF2 | VR2 | AR2 |
| CYLND3 | RINGNO3 | NMMA3 | CF3 | VR3 | AR3 |

Two-Stroke-Cycle Gasoline Engine Lubricant Evaluation

D4857 (Y350M2) ASTM TC Sequence I Test Procedure

Operational Summary

Form 7

| Lab LAB | EOT Date DTCOMP | End Time EOTTIME |
| --- | --- | --- |
| Engine No. ENGINE | Run Number ENRUN |
| Reference Oil CMIR CYLROCDE | Industry Oil Code IND | Cylinder |
| Non Reference Oil OILCODE CYLOILCD | Cylinder |
| Formulation / Stand Code FORM |

| Parameters | Phase I | Phase II |
| --- | --- | --- |
|  | Maximum | Minimum | Average | Maximum | Minimum | Average |
| Engine Speed, r/min | XRPM1 | IRPM1 | ARPM1 | XRPM2 | IRPM2 | ARPM2 |
| Dynamometer Speed, r/min | XDYNRPM1 | IDYNRPM1A | DYNRPM1 | XDYNRPM2 | IDYNRPM2A | ADYNRPM2 |
| Observed Load, hp | XOBLOAD1 | IOBLOAD1 | AOBLOAD1 | XOBLOAD2 | IOBLOAD2 | AOBLOAD2 |
| Corrected Load, hp | XCOLOAD1 | ICOLOAD1 | ACOLOAD1 | XCOLOAD2 | ACOLOAD2 | ICOLOAD2 |
| Air / Fuel Ratio - Baseline | RXAFRAT1 | RIAFRAT1 | RAAFRAT1 | RXAFRAT2 | RIAFRAT2 | RAAFRAT2 |
| Air / Fuel Ratio - Test Oil | XAFRAT1 | IAFRAT1 | AAFRAT1 | XAFRAT2 | IAFRAT2 | AAFRAT2 |
| Air Flow lb / h - Baseline | RXAFLOW1 | RIAFLOW1 | RAAFLOW1 | RXAFLOW2 | RIAFLOW2 | RAAFLOW2 |
| Air Flow lb / h - Test Oil | XAFLOW1 | IAFLOW1 | AAFLOW1 | XAFLOW2 | IAFLOW2 | AAFLOW2 |
| Fuel Flow lb / h - Baseline | RXFFLOW1 | RIFFLOW1 | RAFFLOW1 | RXFFLOW2 | RIFFLOW2 | RAFFLOW2 |
| Fuel Flow lb / h - Test Oil | XFFLOW1 | IFFLOW1 | AFFLOW1 | XFFLOW2 | IFFLOW2 | AFFLOW2 |
| Pressures |  |  |  |  |  |  |
| Fuel Pressure, psi - Baseline | RXFUELP1 | RIFUELP1 | RAFUELP1 | RXFUELP2 | RIFUELP2 | RAFUELP2 |
| Fuel Pressure, psi - Test Oil | XFUELP1 | IFUELP1 | AFUELP1 | XFUELP2 | IFUELP2 | AFUELP2 |
| Intake Air Pressure, in. H2O | XINAIRP1 | IINAIRP1 | AINAIRP1 | XINAIRP2 | IINAIRP2 | AINAIRP2 |
| Barometric Pressure, in. Hg | XBAROP1 | IBAROP1 | ABAROP1 | XBAROP2 | IBAROP2 | ABAROP2 |
| Temperatures,° F |  |  |  |  |  |  |
| Spark Plug - Baseline | RXSPKPT1 | RISPKPT1 | RASPKPT1 | RXSPKPT2 | RISPKPT2 | RASPKPT2 |
| Spark Plug - Test Oil | XSPKPT1 | ISPKPT1 | ASPKPT1 | XSPKPT2 | ISPKPT2 | ASPKPT2 |
| Cylinder Liner - Baseline | RXCYLLT1 | RICYLLT1 | RACYLLT1 | RXCYLLT2 | RICYLLT2 | RACYLLT2 |
| Cylinder Liner- Test Oil | XCYLLT1 | ICYLLT1 | ACYLLT1 | XCYLLT2 | ICYLLT2 | ACYLLT2 |
| Exhaust - Baseline | RXEXHT1 | RIXEXHT1 | RAEXHT1 | RXEXHT2 | RIXEXHT2 | RAEXHT2 |
| Exhaust - Test Oil | XEXHT1 | IEXHT1 | AEXHT1 | XEXHT2 | IEXHT2 | AEXHT2 |
| Fuel - Baseline | RXFUELT1 | RIFUELT1 | RAFUELT1 | RXFUELT2 | RIFUELT2 | RAFUELT2 |
| Fuel - Test Oil | XFUELT1 | IFUELT1 | AFUELT1 | XFUELT2 | IFUELT2 | AFUELT2 |
| Intake Air, Carburetor | XINAIRT1 | IINAIRT1 | AINAIRT1 | XINAIRT2 | IINAIRT2 | AINAIRT2 |
| Intake Air Dew Point | XINDWPT1 | IINDWPT1 | AINDWPT1 | XINDWPT2 | IINDWPT2 | AINDWPT2 |
| Ambient | XINAMBT1 | IINAMBT1 | AINAMBT1 | XINAMBT2 | IINAMBT2 | AINAMBT2 |

Two-Stroke-Cycle Gasoline Engine Lubricant Evaluation

D4857 (Y350M2) ASTM TC Sequence I Test Procedure

Remarks and Deviations

Form 8

| Lab LAB | EOT Date DTCOMP | End Time EOTTIME |
| --- | --- | --- |
| Engine No. ENGINE | Run Number ENRUN |
| Reference Oil CMIR CYLROCDE | Industry Oil Code IND | Cylinder |
| Non Reference Oil OILCODE CYLOILCD | Cylinder |
| Formulation / Stand Code FORM |

| Other Comments |
| --- |
| Number of Comment TOTCOM |  |  |

Two-Stroke-Cycle Gasoline Engine Lubricant Evaluation

D4857 (Y350M2) ASTM TC Sequence I Test Procedure

Remarks and Deviations

Form 8A

| Lab LAB | EOT Date DTCOMP | End Time EOTTIME |
| --- | --- | --- |
| Engine No. ENGINE | Run Number ENRUN |
| Reference Oil CMIR CYLROCDE | Industry Oil Code IND | Cylinder |
| Non Reference Oil OILCODE CYLOILCD | Cylinder |
| Formulation / Stand Code FORM |

| Other Comments |
| --- |
| Number of Comment TOTCOM |  |  |

Two-Stroke-Cycle Gasoline Engine Lubricant Evaluation

D4857 (Y350M2) ASTM TC Sequence I Test Procedure

Remarks and Deviations

Form 8B

| Lab LAB | EOT Date DTCOMP | End Time EOTTIME |
| --- | --- | --- |
| Engine No. ENGINE | Run Number ENRUN |
| Reference Oil CMIR CYLROCDE | Industry Oil Code IND | Cylinder |
| Non Reference Oil OILCODE CYLOILCD | Cylinder |
| Formulation / Stand Code FORM |

| Other Comments |
| --- |
| Number of Comment TOTCOM |  |  |

Two-Stroke-Cycle Gasoline Engine Lubricant Evaluation

D4857 (Y350M2) ASTM TC Sequence I Test Procedure

Phase II Air Fuel Ratio Plots

Form 9

| Lab | EOT Date DTCOMP | End Time EOTTIME |
| --- | --- | --- |
| Engine No. ENGINE | Run Number ENRUN |
| Reference Oil CMIR CYLROCDE | Industry Oil Code IND | Cylinder |
| Non Reference Oil OILCODE CYLOILCD | Cylinder |
| Formulation / Stand Code FORM |

##### AFRATIM

Two-Stroke-Cycle Gasoline Engine Lubricant Evaluation

D4857 (Y350M2) ASTM TC Sequence I Test Procedure

Phase II Spark Plug Plots

Form 10

| Lab LAB | EOT Date DTCOMP | End Time EOTTIME |
| --- | --- | --- |
| Engine No. ENGINE | Run Number ENRUN |
| Reference Oil CMIR CYLROCDE | Industry Oil Code IND | Cylinder |
| Non Reference Oil OILCODE CYLOILCD | Cylinder |
| Formulation / Stand Code FORM |

##### SPKPTIM

Two-Stroke-Cycle Gasoline Engine Lubricant Evaluation

D4857 (Y350M2) ASTM TC Sequence I Test Procedure

Test Fuel Analysis (Last Batch)

Form 11

| Lab LAB | EOT Date DTCOMP | End Time EOTTIME |
| --- | --- | --- |
| Engine No. ENGINE | Run Number ENRUN |
| Reference Oil CMIR CYLROCDE | Industry Oil Code IND | Cylinder |
| Non Reference Oil OILCODE CYLOILCD | Cylinder |
| Formulation / Stand Code FORM |
| Supplier FUELSP | Batch Identifier FUELBTID |

| Measurement | Specs. | Analysis | Test Method |
| --- | --- | --- | --- |
| Gravity, °API | Report | APIGRNEW | D 1250 |
| Copper Corrosion, 3h @ 50 °C | 1 Maximum | FUELCU | D 130 |
| Reid Vapor Pressure, psig | Report | FUELREID | D 5191 |
| Research Octane Number | Report | ROCTANEN | D 2699 |
| Motor Octane Number | Report | MOCTANEN | D 2700 |
| (Research + Motor) / 2 | Report | RMOTOR2 |  |
| Total Sulfur, ppm | 125 Max | FUELSNEW | D 2622 |
| Gum, mg/100 mL | Report | FUELGUM | D 381 |
| Distillation, °C |  |  |  |
| IBP | Report | FUELIBP | D 86 |
| 10% | Report | FUEL10 | D 86 |
| 50% | Report | FUEL50 | D 86 |
| 90% | Report | FUEL90 | D 86 |
| EP | Report | FUELEP | D 86 |
| Recovery, % | Report | FUELRECO | D 86 |
| Pona, % vol |  |  |  |
| Paraffins + Napthenes | Report | FUELPN | D 1319 |
| Olefin | 10 – 15 | FUELOLEF | D 1319 |
| Aromatics % Vol. | 28 – 33 | FUELAROM | D 1319 |

# Text boxes

A A correction factor of -1.85 merits is applied to the benchmark reference oil (TMC 606) second ring sticking results,

when run with the non-reference oil.

B The adjusted ring rating is calculated  by averaging the  NMMA ring rating and the visual  ring rating. The visual	ring

rating is calculated by assessing  the total  number of  degrees the  ring visually  appears  to be stuck in the  groove.	The

normal NMMA ring ratings are then applied as though the ring is firmly stuck over the area, even though in most cases

rings in this condition can be forced to move through the application of varying amounts of pressure.