Sequence VG Report Forms

Version  VERSION

Conducted For

## TSTSPON1

TSTSPON2

| LABVALID | V = Valid |
| --- | --- |
|  | I = Invalid |
|  | N = Results cannot be interpreted as representative of oil performance (Non-Reference Oil) and shall not be used in determining an average test result using multiple test acceptance criteria. |

| TSTOIL | NR = Non-reference Oil Test |
| --- | --- |
|  | RO = Reference Oil Test |

| Test Number |
| --- |
| Stand: STAND | Runs Between Calibration Tests: STRUN | Total Runs on Stand: TOTSRUN |
| Date Completed: DTCOMP | End of Test Time: EOTTIME |
| Oil Code: OILCODE |
| Formulation/Stand Code: FORM |
| Alternate Codes: | ALTCODE1 | ALTCODE2 | ALTCODE3 |

In my opinion this test OPVALID has been conducted in a valid manner in accordance with the VG Test Method D 6593 and the appropriate amendments through the Information Letter system. The remarks included in the report describe the anomalies associated with this test.

SUBLAB

Testing Laboratory

SUBSIGIM

Signature

SUBNAME

Typed Name

SUBTITLE

Title

SUBMITTED BY

Form 2

Sequence VG

##### Table of Contents

1.	Title / Validity Declaration Page	Form 1

2.	Table of Contents	Form 2

3.	Summary of Test Method	Form 3

4.  	Test Result Summary	Form 4

5.	Test Result Summary	Form 5

6.	Operational Summary	Form 6

7.	Oil Addition Record & Blowby Rates	Form 7

8.	Analysis of Oil	Form 8

9.	Downtime Occurrences and Other Comments	Form 9

10.	ACC Conformance Statement	Form 10

Sequence VG Sludge and Varnish Deposit Test

Form 3

Summary of Test Method

The Sequence VG engine sludge and varnish deposit test is a fired engine-dynamometer test which evaluates the  ability  of  a  lubricant  to minimize the formation of sludge and varnish deposits.  This test method is a cyclic test, with a total running duration of 216 hours.

The test engine is a Ford 4.6L, spark ignition, four stroke, eight cylinder “V” configuration engine.  Features of this engine include dual overhead camshafts, a cross-flow fast burn cylinder head design, two valves per cylinder and electronic port fuel injection.  A 90 minute break-in schedule is conducted prior to each test, since a new engine build is used for each test.

The Sequence VG test requires a new engine for each test.  Each test is run for 216 hours, consisting of 54 cycles of 4 hours each.  Each cycle consists of 3 stages.  The stages of the test cycle are set at the following conditions:

| Condition | Stage I | Stage II | Stage III |
| --- | --- | --- | --- |
| Duration, minutes | 120 | 75 | 45 |
| Engine Speed, r/min | 1200 | 2900 | 700 |
| Engine Power, kW | Record | Record | 1.10 - 1.50 |
| Manifold Abs Press, kPa (abs) | 69 | 66 | Record |
| Engine Oil In, oC | 68 | 100 | 45 |
| Engine Coolant Out, oC | 57 | 85 | 45 |
| Engine Coolant Flow, L/min | 48 | Record | Record |
| Engine Coolant Pressure, kPa (gauge) | 70 | 70 | 70 |
| RAC Coolant In, oC | 29 | 85 | 29 |
| Rocker Cover Flow, L/min | 15 | 15 | 15 |
| Intake Air, oC | 30 | 30 | 30 |
| Intake Air, Press, kPa (gauge) | 0.05 | 0.05 | 0.05 |
| Exhaust Gas Analysis, Lambda | 1.0 | 1.0 | 0.75 |
| Blowby Flow Rate Avg, L/min | Record | 60 - 70 | ----- |
| Air/Fuel Ratio | Stoichmetric | Stoichmetric | 11.5:1 |
| Intake Air Humidity, g/kg | 11.4 | 11.4 | 11.4 |
| Exhaust Back Pressure, kPa abs | 104 | 107 | Record |
| Fuel Flow, kg/h | Record | Record | Record |

Upon test completion, the engine is disassembled and rated for sludge and varnish.  Average Engine Sludge and Average Engine Varnish are calculated.

Sequence VG

Form 4

Test Result Summary

Non-Reference & Reference Oil Tests

| Laboratory: LAB | Stand: STAND | Stand Runs: STRUN | Total Runs on Stand:TOTSRUN |
| --- | --- | --- | --- |
| Oilcode: OILCODE |
| Formulation/Stand Code: FORM |

| Date Started: DTSTRT | Time Started: STRTTIME |
| --- | --- |
| Lab Engine Number: ENGINE | SAE Viscosity: SAEVISC |
| Test Length: TESTLEN | Fuel Batch: FUELBTID |
| Industry Oil Code: IND |  |

| Critical Parameters |
| --- |
|  | Average Engine Sludge, merits | Rocker Cover Sludge, merits | Average Engine Varnish, merits | Average Piston Skirt Varnish, merits | Oil Screen Sludge, % Area | Number of Hot Stuck Rings |
| Original Result | AES | RACS | AEVB | APV | OSCRNSLG | NHSCMPRG |
| Transformed Result |  |  |  |  | TRANOSCR |  |
| Industry Correction Factor | AESCF | RACSCF | AEVBCF | APVCF | TOSCRCF | NHSRCF |
| Corrected Transformed Result |  |  |  |  | TOSCRCOR |  |
| Severity Adjustment | AESSA | RACSSA | AEVBSA | APVSA | TOSCRSA | NHSRSA |
| Final Transformed Result |  |  |  |  | TOSCRFNL |  |
| Final Original Unit Result | AESFNL | RACSFNL | AEVBFNL | APVFNL | OSCRFNL | NHSRFNL |

| Clogging Information | Additional Information |
| --- | --- |
| Oil Screen Debris, % Area | OSCRNDEB | Number of Cold Stuck Rings | NCSCMPRG |
| Oil Ring Clogging, % Area | OILRING | Average Blowby Stage II, L/min | ACBLWRT2 |
| PCV Valve @ 25 kPa, % | PCV25 | Oil Consumption, grams | TOILCONS |
| PCV Valve @ 60 kPa, % | PCV60 |  |

| Last Reference Oil Test Calibrating Stand Information – Fill Out For Non-reference Oil Tests Only |
| --- |
| Stand: RSTAND | Total Runs on Test Stand RTOTSRUN |
| Oilcode: ROILCODE |
| Industry Oil Code: RIND | Engine Number: RENGINE | SAE Viscosity: RSAEVISC | Date Completed: RDTCOMP |
| Test Length: RTESTLEN | Fuel Batch: RFUELBID | Calibration Expiration Date: RDTCALEX |
| Clogging Information | Additional Information |
| Oil Screen Debris, % Area | ROSCRDEB | Number of Cold Stuck Rings | RCSCMPRG |
| Oil Ring Clogging, % Area | ROILRING | Average Blowby Stage II, L/min | RACBLWR2 |
| PCV Valve @ 25 kPa, % | RPCV25 | Oil Consumption, grams | RTOILCON |
| PCV Valve @ 60 kPa, % | RPCV60 |  |
|  | Average Engine Sludge, merits | Average Rocker Cover Sludge, merits | Average Engine Varnish, merits | Average Piston Skirt Varnish, merits | Oil Screen Sludge, % Area | Number of Hot Stuck Rings |
| Final Original Unit Result | RAESFNL | RRACSFNL | RAEV3FNL | RAPVFNL | ROSCRSLG | RHSCMPRG |

Sequence VG

Form 5

Test Result Summary

Non-Reference & Reference Oil Tests

| Laboratory: LAB | Stand: STAND | Stand Runs: STRUN | Total Runs on Stand:TOTSRUN |
| --- | --- | --- | --- |
| Oilcode: OILCODE |
| Formulation/Stand Code: FORM |

| Hardware Identification | Production Number PRODNUM | Serial Number SERNUM |
| --- | --- | --- |
| Casting Numbers | Block BLKCAST | Cam, Left CAMCASTL | Cam, Right CAMCASTR |
| Piston Part Number PISTPART | Piston Ring Casting Number PRINGNUM |
| Cylinder Head Casting Number | Left CYLHCSTL | Right CYLHCSTR |

| Varnish Deposits |
| --- |
| Area | Merit |
| Piston Skirt, Thrust | APV |
| Rocker Arm Cover, Left | CAMBLVRT |
| Rocker Arm Cover, Right | CAMBRVRT |
| Average Engine Varnish | AEVB |

| Sludge Deposits |
| --- |
| Area | Merit |
| Rocker Arm Cover, Left | RACLSRT |
| Rocker Arm Cover, Right | RACRSRT |
| Camshaft Baffle, Left | CAMBLSRT |
| Camshaft Baffle, Right | CAMBRSRT |
| Timing Chain Cover | TCCSRT |
| Oil Pan Baffle | OILPBSRT |
| Oil Pan | OILPNSRT |
| Valve Deck Area, Left | VLVDLSRT |
| Valve Deck Area, Right | VLVDRSRT |
| Average Engine Sludge | AES |
| Piston Varnish Deposits, Thrust Side |
| Piston Number | Merit |
| 1 | PSVTH1 |
| 2 | PSVTH2 |
| 3 | PSVTH3 |
| 4 | PSVTH4 |
| 5 | PSVTH5 |
| 6 | PSVTH6 |
| 7 | PSVTH7 |
| 8 | PSVTH8 |
| Average | APV |

| Wear Measurements |
| --- |
| Ring Wear | Units | Value |
| Follower Pin Wear, cyl #8, Intake | µm | CFPIN8I |
| Follower Pin Wear, cyl #8, Exhaust. | µm | CFPIN8E |
| Ring Gap Increase, cyl #1 & #8, Max | µm | MXRGINC |
| Ring Gap Increase, cyl #1 & #8, Avg | µm | ARGINC |

Sequence VG

Form 6

#### Operational Summary

| Laboratory: LAB | Stand: STAND | Stand Runs: STRUN | Total Runs on Stand:TOTSRUN |
| --- | --- | --- | --- |
| Oilcode: OILCODE |
| Formulation/Stand Code: FORM |

| Controlled Parameters | Parameter | Units | QI Threshold | EOT QI | Target | Average | Samples | BQD | Over/Under Range |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Stage 1 | Stage 2 | Stage 3 | Stage 1 | Stage 2 | Stage 3 |  |  |  |
|  | Speed | r/min | 0.000 | QRPM | 1200 | 2900 | 700 | ARPM1 | ARPM2 | ARPM3 | NRPM | BRPM | ORPM |
|  | Manifold Abs Press | kPa | 0.000 | QMANABP | 69 | 66 | Record | AMANABP1 | AMANABP2 | AMANABP3 | NMAP | BMAP | OMAP |
|  | Engine Oil, In | oC | 0.000 | QENGOIN | 68 | 100 | 45 | AENGOIN1 | AENGOIN2 | AENGOIN3 | NEOIN | BEOIN | OEOIN |
|  | Engine Coolant, Out | oC | 0.000 | QCOLOUT | 57 | 85 | 45 | ACOLOUT1 | ACOLOUT2 | ACOLOUT3 | NCOUT | BCOUT | OCOUT |
|  | Engine Coolant Flow | L/min | 0.000 | QCOLFRT | 48 | Record | Record | ACOLFRT1 | ACOLFRT2 | ACOLFRT3 | NCFRT | BCFRT | OCFRT |
|  | Engine Coolant Pressure | kPa | 0.000 | QCOLPRE | 70 | 70 | 70 | ACOLPRE1 | ACOLPRE2 | ACOLPRE3 | NCPRE | BCPRE | OCPRE |
|  | RAC Coolant, In | oC | 0.000 | QRACCTP | 29 | 85 | 29 | ARACCTP1 | ARACCTP2 | ARACCTP3 | NRACC | BRACC | ORACC |
|  | RAC Flow | L/min | 0.000 | QRACCFR | 15 | 15 | 15 | ARACCFR1 | ARACCFR2 | ARACCFR3 | NRACF | BRACF | ORACF |
|  | Intake Air | oC | 0.000 | QINAIRT | 30 | 30 | 30 | AINAIRT1 | AINAIRT2 | AINAIRT3 | NINAT | BINAT | OINAT |
|  | I Intake Air Pressure | kPa | 0.000 | QINAIRP | 0.05 | 0.05 | 0.05 | AINAIRP1 | AINAIRP2 | AINAIRP3 | NINAP | BINAP | OINAP |
|  | Intake Air Humidity | g/kg | 0.000 | QAIRHUM | 11.4 | 11.4 | 11.4 | AAIRHUM1 | AAIRHUM2 | AAIRHUM3 | NAHUM | BAHUM | OAHUM |
|  | Exhaust Backpressure | kPa | 0.000 | QEXBKPR | 104 | 107 | Record | AEXBKPR1 | AEXBKPR2 | AEXBKPR3 | NEXBP | BEXBP | OEXBP |
| Non-controlled Parameters pParameters Parameters | Parameter | Units |  | Specifications |  |  |  |  |
|  | Fuel Flow | kg/h |  | Record | Record | Record | AFUELRT1 | AFUELRT2 | AFUELRT3 |  |
|  | Blowby | L/min |  | Record | 60-70 |  |  | ACBLWRT2 |  |  |
|  | Power | kW |  | Record | Record | 1.3 ± 0.2 | APOWER1 | APOWER2 | APOWER3 |  |
|  | Exhaust Gas |  |  |  |  |  |  |  |  |  |
|  | Lambda, Left Bank | AFR |  | 1.0 | 1.0 | 0.75 | LLAMBDA1 | LLAMBDA2 | LLAMBDA3 |  |
|  | Lambda, Right Bank | AFR |  | 1.0 | 1.0 | 0.75 | RLAMBDA1 | RLAMBDA2 | RLAMBDA3 |  |

Sequence VG

Form 7

Oil Addition Record & Blowby Rates

Non-Reference & Reference Oil Tests

| Laboratory: LAB | Stand: STAND | Stand Runs: STRUN | Total Runs on Stand:TOTSRUN |
| --- | --- | --- | --- |
| Oilcode: OILCODE |
| Formulation/Stand Code: FORM |

| Cycle | Test Hour | Oil Added, g | Oil Consumed, g |
| --- | --- | --- | --- |
| CYC_R006 | TSC_R006 | OILAR006 | OILCR006 |
| CYC_R012 | TSC_R012 | OILAR012 | OILCR012 |
| CYC_R018 | TSC_R018 | OILAR018 | OILCR018 |
| CYC_R024 | TSC_R024 | OILAR024 | OILCR024 |
| CYC_R030 | TSC_R030 | OILAR030 | OILCR030 |
| CYC_R036 | TSC_R036 | OILAR036 | OILCR036 |
| CYC_R042 | TSC_R042 | OILAR042 | OILCR042 |
| CYC_R048 | TSC_R048 | OILAR048 | OILCR048 |
| CYC_R054 | TSC_R054 |  | OILCR054 |
| Total, g | TOILADD | TOILCONS |

| Stage II |
| --- |
| Test Hours | Blowby, L/min |
| TSBBRK | BLBYBRK |
| TSB_H023 | BLBYH023 |
| TBS_H047 | BLBYH047 |
| TBS_H071 | BLBYH071 |
| TBS_H095 | BLBYH095 |
| TBS_H119 | BLBYH119 |
| TBS_H143 | BLBYH143 |
| TSB_H167 | BLBYH167 |
| TBS_H191 | BLBYH191 |
| TBS_H215 | BLBYH215 |
| Maximum | XCBLWRT2 |
| Minimum | MCBLWRT2 |
| Average Blowby, Hours 23 - 119 | ABLW2120 |
| Average | ACBLWRT2 |

Sequence VG

Form 8

Analysis of Oil

| Laboratory: LAB | Stand: STAND | Stand Runs: STRUN | Total Runs on Stand:TOTSRUN |
| --- | --- | --- | --- |
| Oilcode: OILCODE |
| Formulation/Stand Code: FORM |

| Test Hours | Ag, ppm | Al, ppm | Cr, ppm | Cu, ppm | Fe, ppm | Pb, ppm | Si, ppm | Sn, ppm | Fuel Dilution by GC, Wt.% D3525 | Pentane Insolubles, Wt.% D893BA | TBN D4739A | Vis. @ 40oC, cSt D445 | Vis. @ 100oC, cSt D445A |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TST_HNEW | GWMHNEW | ALWMHNEW | CRWMHNEW | CUWMHNEW | FEWMHNEW | PBWMHNEW | SIWMHNEW | SNWMHNEW |  |  | TBN_HNEW | V40_HNEW | V100HNEW |
| TST_H024 | AGWMH024 | ALWMH024 | CRWMH024 | CUWMH024 | FEWMH024 | PBWMH024 | SIWMH024 | SNWMH024 | FUELH024 |  | TBN_H024 | V40_H024 | V100H024 |
| TST_H048 | AGWMH048 | ALWMH048 | CRWMH048 | CUWMH048 | FEWMH048 | PBWMH048 | SIWMH048 | SNWMH048 | FUELH048 | PEN_H048 | TBN_H048 | V40_H048 | V100H048 |
| TST_H072 | AGWMH072 | ALWMH072 | CRWMH072 | CUWMH072 | FEWMH072 | PBWMH072 | SIWMH072 | SNWMH072 | FUELH072 |  | TBN_H072 | V40_H072 | V100H072 |
| TST_H096 | AGWMH096 | ALWMH096 | CRWMH096 | CUWMH096 | FEWMH096 | PBWMH096 | SIWMH096 | SNWMH096 | FUELH096 | PEN_H096 | TBN_H096 | V40_H096 | V100H096 |
| TST_H120 | AGWMH120 | ALWMH120 | CRWMH120 | CUWMH120 | FEWMH120 | PBWMH120 | SIWMH120 | SNWMH120 | FUELH120 |  | TBN_H120 | V40_H120 | V100H120 |
| TST_H144 | AGWMH144 | ` ALWMH144 | CRWMH144 | CUWMH144 | FEWMH144 | PBWMH144 | SIWMH144 | SNWMH144 | FUELH144 | PEN_H144 | TBN_H144 | V40_H144 | V100H144 |
| TST_H168 | AGWMH168A AGWMH168 | ALWMH168 | CRWMH168 | CUWMH168 | FEWMH168 | PBWMH168 | SIWMH168 | SNWMH168 | FUELH168 |  | TBN_H168 | V40_H168 | V100H168 |
| TST_H192 | AGWMH192 | ALWMH192 | CRWMH192 | CUWMH192 | FEWMH192 | PBWMH192 | SIWMH192 | SNWMH192 | FUELH192 | PEN_H192 | TBN_H192 | V40_H192 | V100H192 |
| TST_H216 | AGWMH216 | ALWMH216 | CRWMH216 | CUWMH216 | FEWMH216 | PBWMH216 | SIWMH216 | SNWMH216 | FUELH216 | PEN_H216 | TBN_H216 | V40_H216 | V100H216 |

A Analyses not required by Test Method

#### Sequence VG

Form 9

Downtime Occurrences and Other Comments

| Laboratory: LAB | Stand: STAND | Stand Runs: STRUN | Total Runs on Stand:TOTSRUN |
| --- | --- | --- | --- |
| Oilcode: OILCODE |
| Formulation/Stand Code: FORM |

| Number of Downtime Occurrences | DWNOCR |  |
| --- | --- | --- |
| Test Hours | Date | Downtime | Reasons |
| DOWNR001 | DDATR001 | DTIMR001 | DREAR001 |
|  |  | TOTLDOWN | Total Downtime |

| Other Comments |
| --- |
| Number of Comment Lines | TOTCOM |  |
| OCOMR001 |

Sequence VG

Form 9A

Downtime Occurrences and Other Comments

| Laboratory: LAB | Stand: STAND | Stand Runs: STRUN | Total Runs on Stand:TOTSRUN |
| --- | --- | --- | --- |
| Oilcode: OILCODE |
| Formulation/Stand Code: FORM |

| Number of Downtime Occurrences | DWNOCR |  |
| --- | --- | --- |
| Test Hours | Date | Downtime | Reasons |
| DOWNR001 | DDATR001 | DTIMR001 | DREAR001 |
|  |  | TOTLDOWN | Total Downtime |

| Other Comments |
| --- |
| Number of Comment Lines | TOTCOM |  |
| OCOMR001 |

Sequence VG

Form 9B

Downtime Occurrences and Other Comments

| Laboratory: LAB | Stand: STAND | Stand Runs: STRUN | Total Runs on Stand:TOTSRUN |
| --- | --- | --- | --- |
| Oilcode: OILCODE |
| Formulation/Stand Code: FORM |

| Number of Downtime Occurrences | DWNOCR |  |
| --- | --- | --- |
| Test Hours | Date | Downtime | Reasons |
| DOWNR001 | DDATR001 | DTIMR001 | DREAR001 |
|  |  | TOTLDOWN | Total Downtime |

| Other Comments |
| --- |
| Number of Comment Lines | TOTCOM |  |
| OCOMR001 |

Sequence VG

Form 10

American Chemistry Council Code Of Practice

Test Laboratory Conformance Statement

| Test Laboratory |  |
| --- | --- |
| Test Sponsor |  |
| Formulation / Stand Code |  |
| Test Number |  |
| Start Date |  | Start Time |  | Time Zone |  |

# Declarations

No. 1	All requirements of the ACC Code of Practice for which the test laboratory is responsible were met in the conduct of this test.   Yes _______     No_______ *

No. 2	The laboratory ran this test for the full duration following all procedural requirements; and all operational validity requirements of the latest version of the applicable test procedure (ASTM or other), including all updates issued by the organization responsible for the test, were met.

Yes ________    No________*

If the response to this Declaration is “No”, does the test engineer consider the deviations from operational validity requirements that occurred to be beyond the control of the laboratory?  Yes ________*    No________

No 3.	A deviation occurred for one of the test parameters identified by the organization responsible for the test as being a special case.  Yes _______*       No________ (This currently applies only to specific deviations identified in the ASTM Information Letter System)

## Check The Appropriate Conclusion

|  | Operational review of this test indicates that the results should be included in the Multiple Test Acceptance Criteria calculations. |
| --- | --- |
|  | *Operational review of this test indicates that the results should not be included in the Multiple Test Acceptance Criteria calculations. |

Note: Supporting comments are required for all responses identified with an asterisk.

Comments

_________________________________                 ________________________________________

Signature                                                                                                       Date

_________________________________                 ________________________________________

Typed Name							               Title