Minutes

ASTM ROBO August 2011 Teleconference, Thursday August 11, 2011 at 10AM EDT

Issued:  October 5, 2011

| Ace Glass | Alan Kramme |
| --- | --- |
| Afton | Monica Brown Shelia Thompson |
| Ashland Valvoline | Amol Savant |
| ASTM TMC | Frank Farber Tom Schofield |
| BP/Castrol | Irwin Goldblatt |
| Chevron Oronite | Mark Sutherland |
| ExxonMobil | Dennis Gaal |
| Intertek Automotive Research | Joe Franklin Matt Schlaff |
| Lubrizol | Rick Hartman Erica Ware |
| RT Vanderbilt | Al Filho |
| Evonik RohMax | Alan Flamberg Justin Mills Joan Souchik |
| SouthWest Research | Mike Birke Becky Grinfield |

AGENDA

1.Welcome

2. Agenda Review

3. June Teleconference Review and Minutes

Minutes:       B.7 presentation:

June minutes approved as distributed.

4. Statistics as of August 9, 2011

ROBO Industry Statistics Based Upon LTMS Data Sets
April Period   =10/1 to 3/31
October Period =4/1 to 9/30
pooled s is by reference material ( example: oil)
                                                 Degrees of      Pooled
  Parameter   Period        N-size  Average Yi      Freedom           s
  ƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒƒ
                                                                       
  MRV          2008OCT          10     -0.3595            7      0.2769
  MRV          2009APR          12     -0.5696            9      0.2229
  MRV          2009OCT          25     -0.6238           22      0.1855
  MRV          2010APR          61     -0.2386           58      0.3941
  MRV          2010OCT         115     -0.2630          111      0.5113
  MRV          2011APR         121      0.2876          118      0.7092
  MRV          2011OCT          67     -0.6718           63      0.2596

April 2011 data contains one ‘outlier’ high result which under current rules would not be included, but remains in the data set as it was not excluded under the rules in place then.  The current precision looks good and we feel it is a result of the recent revision of our rules and testing practices.

5. 435-2 Update

| LAB | APP | 435 CMIR | 435 MRV | 435 ln (MRV) | 435-2 CMIR | 435-2 MRV | 435-2 ln (MRV) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| AM | AM3 |  |  |  | 80546 | 65400 | 11.0882775 | Screener |
| AM | AM4 |  |  |  | 80547 | 50700 | 10.8336812 | Screener |
| G | G5 |  |  |  | 80548 | 88900 | 11.3952674 | Screener |
| A | A2 | 74468 | 52900 | 10.8761586 | 81693 | 61000 | 11.0186291 | Calibration Failed Mild |
| A | A3 | 74459 | 62700 | 11.0461167 | 81694 | 54600 | 10.9077892 | run in reverse order |
| AM | AM3 | 82397 | 66400 | 11.1034523 | 81679 | 52700 | 10.8723707 |  |
| AM | AM4 | 73666 | 88600 | 11.3918871 | 81677 | 61300 | 11.0235351 |  |
| AM | AM5 | 73667 | 71300 | 11.1746516 | 81678 | 57000 | 10.9508065 |  |
| AO | AO1 | 70128 | 63899 | 11.065059 | 81658 | 52692 | 10.8722189 |  |
| B | B1 | 74244 | 67300 | 11.1169155 | 81671 | 99000 | 11.5028751 |  |
| B | B2 | 75036 | 109000 | 11.5991032 | 81674 | 64300 | 11.0713149 |  |
| D | D2 | 72584 | 111415 | 11.6210172 | 81664 | 83757 | 11.335675 |  |
| G | G1 | 75045 | 64000 | 11.0666384 | 81649 | 66700 | 11.1079602 |  |
|  |  |  | Average | 11.2427601 | Red Values |  | 11.0801477 | Red & Blue Values |
|  |  |  | exp (cSt) | 76325 |  |  | 64870 |  |
|  |  |  | sR | 0.23276736 |  |  | 0.22177051 |  |

| 435 Target Mean (ln) | 11.4895 |
| --- | --- |
| 435 target Mean (MRV, cSt) | 97685 |
| 435 Target sR |  | 0.2932 |
| 435-1 Target Mean (ln) | 11.0413 |
| 435-1 target Mean (MRV, cSt) | 62420 |
| 435-1 Target sR |  | 0.20295 |

Do we have enough data?  Consensus: include the 12 data points and wait until we reach 15 total before final resolution.

Options for setting the lower limit.

Using red and blue (12 data points each oil)

A.  -1.66 std dev = 44,892

B.  using mean delta (ln(76325)-ln(64870)) subtract from 60,000 limit and get

50,995

(which corresponds to -1.085 st dev)

Compared to limit on 35-1 of 44,570.

3The minimum value for reference oil 435-1 is based on -1.66 standard deviations from the target mean (to match the range previously approved for oil 435 min), so is not actually a 95% confidence range. A 95% confidence range would use 1.96 standard deviations from target mean.

Discussion:

Divided opinions on two options for setting lower limit.  Also concern that 435-2 does not appear to be that different than 435-1 in terms of ROBO MRV results.  We would like to stay aligned with the Sequence IIIG program where 435-2 may be a better test oil than 435-1.  We coordinate with the Sequence IIIG group and are interested in seeing their MRV data when available.

6. New Test Stand Calibration

March:

Discussion: We understand there is a difference between a new lab or a new rig in a lab, and a rig that has been in operation for a while and finds itself requiring 2 tests because of some change or now 2 unsuccessful attempts at certification.  Tom will begin more rigorous enforcement of the practice of demonstrating the new rig can successfully run the 3 TMC oils.  A new rig will need to run the 3 oils, not blind.  The results will be posted in the TMC database and reviewed by the Surveillance Panel (or a subgroup of the Panel if we so choose), before an OK is given to proceed with Certification.  This was what was done for the original ROBO round robin and seems to have lead to repeatable testing on those rigs.

April:

Other Discussion Item:  At the March meeting we discussed the need to demonstrate the ability to acceptably run the three different ASTM TMC reference oils on a new rig before it could be certified.  However, it was pointed out, that we did not reach a consensus on how to go about generating these three runs.  We need to resolve this and a written ballot may be in order.

Consensus:  all three oils need to be run successfully (within TMC statistical limits) for a rig to be accepted.  For the rules, we propose at least one oil (not blind) needs to be run and reported, followed by the 2 oil blind certification.  These need to be coordinated with the TMC as one of the 2 blind oils must be from the 435 series and all three oils must be included.  For a lab new to ROBO, running all three oils (not blind) is recommended, followed by the 2 oil blind certification.

Action:  Joe Franklin will draft the wording to add this practice to the rules, circulate to a small group for editing and discussion (Alan, Tom, and anyone else who would like to be involved at this stage), and then we will take a written vote.

7. Reference/Calibration oil availability

Issue:  The TMC supplies oils for the purpose of monitoring tests of importance to the industry.  The TMC does not supply oils to those outside the TMC monitoring system for tests that are monitored.  Our method implies that these oils are available to all.  That may not be the case.

Decision:  Remove the last sentence of 9.2.  Tom will draft an information letter for us to vote on.  Other editing of the method (perhaps the removal of Table 1 and a reference to current TMC oils and limits) will be considered, but not voted on right now.

NOTE (10/5):  In reviewing a draft of these minutes, it was not clear to all whether we intended to remove the last sentence of 9.2 or to delete the entire paragraph 9.2.  Also a question was raised whether the information letter needed a vote of if it should just be issued.  As there is some confusion, we will resolve this at our next meeting.

8.  Schedule next meeting:  Thursday October 6, 2011 at 10:00 AM Eastern Time.

NOTE (10/5):  Meeting postponed.  Will attempt to reschedule later in the month of October (10/18 target).

9. Adjourn  11:15 AM EDT