## Slide 1: New Liner and Ring Batch Effects in the Mack T-12
Presented to Mack Surveillance Panel
Conference Call
20101103
Jim Rutherford

## Slide 2: Summary
Pb (3 of 4) and Pb2 (2 of 4) higher with T batch rings
CLW dropped, not rings and liners – correction factor needed?
OC higher with T rings
Higher Fe with newer parts?
Different profiles?
No effect on MRV100

## Slide 3: T12: Liner and Ring Batches
Pb higher

## Slide 4
T12: Ring and Liner Batches
Pb2 higher

## Slide 5: T12: Liner and Ring Batches
CLW dropped, not rings and liners.

## Slide 6: T12: Liner and Ring Batches
TRWL hard to tell

## Slide 7: T12: Liner and Ring Batches
OC higher with T rings

## Slide 8: T12: Liner and Ring Batches
Mack merits lower?

## Slide 9: T12: Liner and Ring Batches
Higher Pb function of OC?

## Slide 10: T12: Liner and Ring Batches
Higher Pb2 function of OC?

## Slide 11: T12: Liner and Ring Batches

## Slide 12: T12: Liner and Ring Batches

## Slide 13: T12: Liner and Ring Batches

## Slide 14: T12: Bearing and Main Batches

## Slide 15: T12: Bearing and Main Batches

## Slide 16: T12: Bearing and Main Batches

## Slide 17: T12: Bearing and Main Batches

## Slide 18: T12: Bearing and Main Batches

## Slide 19: T12: Bearing and Main Batches

## Slide 20: T12: Liner and Ring Batches
The correction factor (osCLW x 0.58) was intended to
bring R batch rings back to target (16.2).

## Slide 21: T12: Bearing and Main Batches
The correction factor (osCLW x 0.58) was intended to
bring R batch rings back to target (16.2).

## Slide 22: T12: Liner and Ring Batches
Higher Fe with newer parts?

## Slide 23: T12: Liner and Ring Batches

## Slide 24: T12: Liner and Ring Batches

## Slide 25: T12: Liner and Ring Batches
ST may be more consistent across
cylinders than historical batches

## Slide 26: T12: Liner and Ring Batches
ST may be more extreme on cylinders 3 and 5 than historical batches

## Slide 27: T12: Liner and Ring Batches

## Slide 28: T12: Bearing and Main Batches