SEQUENCE VG AVERAGE ENGINE VARNISH INDUSTRY ALARM LOG

March 9, 2000 to May 13, 2000 (Precision)

Precision EWMA warning and action alarms begin on 3/9/00 and continue on 3/11/00 and 3/16/00. One test was –3.667 (/s from target. Test prior to the start of the alarm event was –0.4167 (/s from target and second test in alarm event was –0.250 (/s from target. A third test completed on 3/16/00 was –1.750. Subsequent results were –2.00, -0.111 and –1.667 (/s from target. Alarm clears when a result on reference oil 1007, -1.35 (/s from target is reported. Precision alarms clear on 5/13/00 and remain in control on 5/25/00, when two results from a new stand are reported consecutively.

March 16, 2000 to May 25, 2000 (Severity, Severe Direction)

Severity EWMA alarm sounds on 3/16/00, when third severe result in series is reported. Three tests were –3.667, -0.250 and –1.750 (/s from target. All three results were from different labs. Subsequent results were –2.00, -0.111 and –1.667 (/s from target, causing an action, a warning and another action alarm to sound. Parameter remains in severity alarm when a result –1.35 (/s from target is reported on reference oil 1007.  Action alarms continue when  test on reference oil 1006, -0.583 (/s from target is reported. Result was from an existing stand. Still in severity warning alarm as of 5/25/00, action alarm cleared on this date. AEVZI is at 0.756, and showing improvement. The last two results were on a new stand, which calibrated. Results from this stand were –0.583 and –0.000 (/s from target with oils 1006 and 1007.

January 20, 2001 to February 17, 2001 (Precision)

A three test warning alarm sounds caused by one test with reference oil 1007 which was –2.556 Δ/s from target followed by tests on 925-3 and 1007, 0.621 and 0.778 Δ/s from target.

Updated: March 20, 2001