L60-1 (Viscosity) INDUSTRY ALARM LOG

November 20, 1995   ( SEVERITY )

One severe warning alarm.  Influenced by two consecutive severe test results from one lab, 1.94 and 3.04 (/s.  Appears to be a lab problem.

November 24, 1995  ( PRECISION )

Two warning alarms occurred.  Not an industry alarm event. The severity event mentioned above and a -1.90 (/s mild result followed by a 2.12 (/s severe result from the lab mentioned above influenced the alarms.

March 31, 1996  (SEVERITY )

One mild warning alarm.  Influenced by two consecutive mild tests from one lab, -2.15 and -3.20 (/s.

September 19, 1997 to October 18, 1997 ( SEVERITY )

One warning and two action alarms occurred during this period.  Not an industry alarm event.   Influenced by three test results from one lab, 1.95, 1.47 and 2.16 (/s severe.

November 1, 1997 to December 5, 1997   ( PRECISION )

A series of three warning and three action alarms occurred during this period.  Alarms were influenced by two tests from two labs, -1.88 and -2.05 (/s mild and two tests from one lab, 1.78 and 1.85 (/s severe.

December 11, 1997 to December 19, 1997  ( SEVERITY )

One action and three warning alarms occurred during this period.  Alarms were influenced by two consecutive test results, 2.30 and 1.47 (/s severe.  These tests were from different labs.

July 9, 199 to July 19, 1998 ( Severity )

Two severe warning alarms occurred during this period. There were no identifiable lab, stand or oil problems. Alarms cleared on next test result.

# November 20, 1998 to March 31, 1999 ( Severity )

There were 13 severe action and four severe warning alarms that occurred during this period.  There were two test results of 4.33 (/s and 3.00 (/s severe from one lab that were responsible for the action alarms.   However, even if these tests are removed, there would still be five severe warning alarms that cannot be traced to any identifiable lab, stand or oil problems.

# June 27, 1999 to August 8, 1999 ( Severity and Precision )

There were seven industry EWMA severity alarms (five warning and two action) and one industry EWMA precision warning alarm this report period. The alarms are related to a chemical analysis problem at one laboratory (Lab D).  The lab is currently working with the TMC to resolve the problem.